# Electronic Properties and Electroluminescent OLED Performance of Panchromatic Emissive N-Aryl-2,3-Naphthalimides

Lili Bao, Yan Zou, Allison Kirk, and Michael D. Heagy*

Department of Chemistry

New Mexico Institute of Mining & Technology

Supplementary Section

Synthesis of the dual fluorescent dyes………………………………………………………..S1

Fluorescence lifetime ………………………………………………………………………..S9

Absorbance maxima of F-OCH3 in solvents of various polarities…….….…………………S13

Fluorescence maxima of F-OCH3 in solvents of various polarities…........………………...S14

Absorbance maxima of F-2OCH3 in solvents of various polarities …………..……………S15

Absorption spectra of dyes in solvents of varying polarities………...……………………..S17

Concentration gradient comparison of absorption spectra for F-2OCH3…………………..S19

Methodology to develop OLED device …………………………………………………………………….S20

References ……………………………………………………………………………………………………………S25

Synthesis of the Compounds:

Schemes 1 though 4 represent the convergent synthetic procedures for preparation of substituted 2,3-naphthalimides. The synthetic methods for preparing 2,3-naphthalimides have been described before.1,2

Scheme 1. Synthesis of substituted 2,3-naphthalic anhydrides (X= fluoro or chloro). Reagents and conditions: (a) zinc in acetic acid, reflux, overnight; (b) DIBAL-H, -78 °C, CH2Cl2; (c) maleic anhydride, acetic acid, reflux; (d) concentrated hydrochloric acid in methanol, reflux.

Scheme 2. Synthetic scheme of N-aryl-2,3-naphthalimides. 
Reagents and conditions: pyridine, 12h

Scheme 3. Synthetic procedure for the preparation of 11. Reagents and conditions: (f) Pd(OAc)2, NaOt-Bu, P(Ph3)4, toluene, refluxing 6 h; (g) hydrogen gas, Pd on activated charcoal, in methanol, 12h.

Scheme 4. Synthesis of disubstituted-2,3-naphthalimide. Reagents and conditions: (h) ethylene glycol, toluene, reflux, overnight; (i) dry DMSO, KOH, ClCH2SO2Ph, overnight, 24 °C; (j) acetic acid/H2O 4:1, reflux 6 h; (k) diethyl maleate, 18-crown-6, K2CO3, CH3CN, reflux, 6 h; (l) p-phenylenediamine, pyridine, reflux, 12 h.

Reduction of phthalic anhydride to lactones: 5 mmol of phthalic anhydride was dissolved in a 100 mL round-bottom flask with 30 mL Acetic acid. To the flask, 5 gram of Zinc dust was added into the flask carefully. The reaction mixture was refluxed overnight with stirring. The reaction mixture was filtered hot, and the residue was rinsed off with 50 mL hot acetic acid twice. Acetic acid from the combined filtrate was removed under reduced pressure. To purify the residues, 100-200 mesh silica gel column chromatography was used with 1% Methanol and 99% dichloromethane as eluting solvents. The yield of the purified product was 88%. 1 and 2 (A): 1H NMR (300 MHz, CDCl3-s): 5.37 (s, 2H), 7.20 (t, 1H, J = 8.0), 7.28 (d, 1H, J = 8.4), 7.68 (d, 1H, J = 4); 13C (300 MHz, CDCl3): 61.4, 126.2, 126.7, 128.4, 129.7, 130.2, 132.2, 134.7, 141.8, 165.5.; 1 and 2 (B): 1H NMR (300 MHz, DMSO-d6): 5.4 (s, 1H), 7.6 (d, 1H, J = 8.2), 7.9 (m, 2H); 13C NMR: 70.1, 123.9, 124.5, 127.2, 129.8, 139.7, 149.9, 170.3.

Reduction of lactones to 1-hydroxyophthalans: 2 mmol) of lactones were dissolved in a 50 mL round-bottom flask with 15 mL dichloromethane. 2 mL (2 mmol) DIBAL-H was added dropwise to the solution at -78 °C. TLC was used to monitor the completion of the reaction. The solution was stirred for 2 h. The reaction mixtures were quenched with methanol, and neutralized with saturated aqueous sodium sulfate solution. The organic layer was extracted with dichloromethane from aqueous solution and the solution was dried over anhydrous sodium sulfate under reduced pressure. The yield was 80%. 3 and 4 (A): 1H NMR (300 MHz, CDCl3-s): 3.32 (d, 1H, J = 6.6), 4.70 (d, 1H, J = 6.6), 5.32 (s, 1H), 6.62 (s, 1H), 7.02 (t, 1H, J = 9.4), 7.08 (d, 1H, J = 7.4), 7.22 (m, 1H); 13C NMR: 69.6, 115.2, 125.2, 126.4, 129, 142.3, 159.3; 3 and 4 (B): 1H NMR (300 MHz, CDCl3-s): 3.39 (d, J = 14.85), 4.8 (dd, 1H, J = 1H), 5.16 (d, 1H, J = 12.9), 6.45 (s, 1H), 7.2 (d, 1H, J = 5.22), 7.3 (d, 1H, J = 4.4), 7.32 (s, 1H); 13C NMR: 68.8, 93.8, 122.6, 123.5, 127.0, 129.9, 148.0.

Diels-Alder reaction between 1-hydroxy phthalans with maleic anhydride: hydroxyl phthalans 2 mmol and maleic anhydride 196 mg (2 mmol) (1:1 ratio) were dissolved in acetic acid and refluxed for 3 h. The reaction mixtures were dried under reduced pressure. The reaction mixtures were purified using column chromatography with 20% ethyl acetate and 80% hexane yielding a mixture of endo and exo products with yield of 65%. 5A: 1H NMR (300 MHz, DMSO-d6): 3.4 (m, 2H), 4.57 (m, 1H), 4.8 (m, 1H), 7.12 (m, 1H), 7.2 (d, 1H, J = 11.5), 7.3 (m, 1H); 13C NMR: 56.7, 63.4, 116.0, 125.4, 125.7, 130.5, 130.9, 137.8, 160, 170.8; 5B: 1H NMR (300 MHz, DMSO-d6): 3.5 (s, 2H), 5.35 (m, 1H), 6.2 (s, 1H), 6.9 (m, 1H), 7.1 (m, 2H); 13C NMR: 49.9, 80.3, 121.7, 128.3, 130.6, 133.7, 140.4, 142.6, 143.8, 168.4, 170.8.

Aromatization of the adducts: The adduct from Diels-Alder reaction 1 mmol was dissolved in a 100-mL round-bottom flask with 25 mL methanol and cHCl (1:4 ratio) and the mixtures were refluxed with stirring overnight. The solutions were neutralized with potassium carbonate and the products were extracted with dichloromethane and concentrated reduced pressure. The products were crystallized in acetic anhydride. 6A: 1H NMR (300 MHz, DMSO-d6): 7.5 (m, 2H), 7.7 (d, 1H, J = 5.8), 7.8 (d, 1H, J = 8.0), 8.3 (s, 1H), 8.4 (s, 1H); 13C NMR: 112.9, 121.8, 125.5, 129.4, 129.5, 130.9, 131.8, 134.8, 156.8, 168.7, 169.0; 6B: 1H NMR (300 MHz, DMSO-d6): 7.7 (d, 1H, J = 8.5), 8.16 (d, 1H, J = 8.8), 8.25 (s, 1H), 8.3 (s, 1H), 8.4 (s, 1H); 13C NMR: 125.3, 126.8, 128.2, 129.1, 130.9, 132.7, 134.5, 135.9, 136.8, 139.7, 144.1, 162.9.

Synthesis of compound (7, 8, and 9): In a 10-mL round-bottom flask, 1 mmol of 2,3-naphthalic anhydride and 1.1 mmol of the 4-substituted aminoarene were dissolved in 5 mL pyridine. The reaction mixture was refluxed for 12 h stirring. Pyridine was removed in the fume hood via stream of air and the residue was filtered using a plug of silica gel with the 30% Ethyl acetate and 70% hexane. Recrystallization was further carried out using ethanol with yield of 85%. 7: 1H NMR (300 MHz, DMSO-d6): 3.8 (s, 3H), 7.0 (d, 2H, J = 8.6), 7.3 (d, 2H, J = 8.8), 7.6 (t, 1H, J = 8.4), 7.8 (d, 1H, J = 8.8), 8.2 (d, 1H, J = 8.6), 8.5 (s, 1H); 13C NMR (300 MHz, DMSO-d6): 56.0, 114.7, 117.1, 125.0, 125.2, 127.2, 129.2, 130.1, 137.2, 159.5, 167.1.; 8: 1H NMR (300 MHz, DMSO-d6): 6.5 (d, 1H, J = 7.6), 6.6 (s, 2H), 6.8 (d, 1H, J = 8.6), 7.3 (d, 2H, J = 8.8), 7.7 (m, 1H), 8.5 (s, 1H); 13C NMR (300 MHz, DMSO-d6): 114.0, 117.8, 124.1, 125.2, 128.7, 129.5, 130.2, 132.7, 134.6, 136.5, 149.3, 167.6. 9, melting point (170 ~ 176 °C): 1H NMR (400 MHz, CDCl3-s): 3.79 (s, 6H), 6.78 (d, 4H, J = 7.88), 6.92 (d, 2H, J = 8.6), 7.04 (d, 3H, J = 7.88), 7.17 (t, 3H, J = 8.28), 7.32 (t, 1H, J = 8.76), 7.58 (t, 1H, J = 3.28), 7.80 (d, 1H, J = 7.88), 8.36 (s, 1H), 8.64 (s, 1H); 13C NMR: 55.5, 113.2, 113.4, 114.8, 118.3, 118.4, 119.7, 123.2, 124.6, 124.62, 125.8, 125.9, 126.0, 127.8, 128.6, 12.4, 129.5, 136.8, 136.9, 140.4, 148.8, 156.3, 158.8, 161.3, and 166.9. FTIR: 1714; 1615; 1504; 1445; 1362; 1331; 1235; 1130 and 1032 cm-1; HRMS found m/z = 519.1707; expected m/z = 519.1720.

Synthesis of compound 4-Methoxyl-N-(4-methoxyl)-N-(4-nitrophenyl)aniline (10): In a 10 mL round-bottom flask, 202 mg of 4-bromonitrobenzene (1 mmol), 275 mg of 4,4’-dimethoxydiphenylamine (1.2 mmol), 2 equivalence of sodium tert-butoxide (200 mg), 5% equivalence palladium acetate (6 mg), and 10% equivalence of triphenylphosphine were added. 5 mL toluene was added into the same flask. With stirring, the mixture was refluxed overnight. TLC was used to monitor the completion of the reaction. After reaction, 15 mL ethyl acetate was used to extract the organic compounds three times. The solvent was removed with aspirator under reduced vacuum, and dark oily product was obtained. To purify the product, column chromatography was used with an eluting solvent of a mixture (8% ethyl acetate and 92% hexane) with yield of 80%. 10 has a melting point of 121~123 ºC. 1H NMR (400 MHz, DMSO-d6, TMS): 3.78 (6H, s), 6.63 (2H, d, J = 12.4 Hz), 7.02 (4H, d, J = 11.7 Hz), 7.27 (4H, d, J = 12.1 Hz), 8.03 (2H, d, J = 12.4 Hz); 13C NMR: 55.54, 115.21, 115.74, 125.61, 128.15, 138.26, 138.95, 154.17, 157.67; FTIR: 1586; 1506; 1496; 1462; 1314; 1286; 1241; 1185; 1110; 1034 and 1024 cm-1; HRMS found m/z = 351.1350, expected m/z = 351.13.

Synthesis of compound N’,N’-bis(4-methoxyphenyl)benzene-1,4-diamine (11): In a 25 mL round-bottom flask, 142 mg (0.4 mmol) of 10 and 5% equivalent (7 mg) Pd/activated carbon catalyst  were added and dissolved in 10 mL methanol. After degassing the solution, a balloon of hydrogen gas was connected to the flask through a syringe needle. The reaction was stirred overnight under room temperature. After the reaction, the solution was filtered and the filtrate was concentrated under reduced vacuum. Dark purple brown power was obtained. Column chromatography was used to purify the product with eluting solvent of 20% ethyl acetate and 80% of hexane. To further purify the product, recrystallization in ethanol was used with a yield of 85%. Melting Point: 110~115 ºC; 1H NMR (400 MHz, CDCl3-d1, TMS): : 3.85 (6H, s), 6.57 (2H, d, J = 8.6 Hz), 6.75 (4H, d, J = 9.0 Hz), 6.86 (2H, d, J = 8.6 Hz), 6.94 (4H, d, J = 9.0 Hz); 13C NMR: 55.54, 114.47, 116.13, 124.32, 125.76, 140.24, 141.80, 142.30, 154.62; FTIR: 3300; 1650; 1450; 1245; and 1030 cm-1; HRMS found m/z = 320.0602; expected m/z = 321.1603.

Synthesis of compound 2-(4-chloro-3-nitrophenyl)-1,3-dioxolane (12): Protection of the aldehyde was performed by following reported procedures271. 4-chloro-3-nitrobenzaldehyde (4.5 g, 24.9 mmol) was dissolved in 250 mL toluene. Ethylene glycol (3.0 mL, 53 mmol) and p-TsOH (150 mg, 0.8 mmol) were added to the solution and the resulting mixture was refluxed overnight with a Dean-stark trap. The solution was concentrated under reduced pressure and the resulting dark solution was purified by chromatography (20% EtOAc/Hexane) to give the desired product with yield of 95%. 1H NMR (300 MHz, CDCl3): 4.0 (s, 4H), 5.82 (s, 1H), 7.17 (d, 1H, J = 7.5), 7.6 (d, 1H, J = 1.5), 7.9 (s, 1H); 13C NMR (300 MHz, CDCl3): 61.0, 61.5, 126.6, 128.4, 129.7, 129.9, 130.1, 132.9, and 142.

Synthesis of compound 2-(4-chloro-3-nitro-2-(phenylsulfonylmethyl)phenyl)-1,3-dioxane (13): 2-(4-chloro-3-nitrophenyl)-1,3-dioxolane (2.0 g, 8.73 mmol) and chloromethyl-phenyl sulfone (1.6 g, 8.73 mmol) were dissolved in dry dimethylsulfoxide. Then, KOH powder (3.2 g) was added to the solution slowly, which turned purple color. The resulting mixture was stirred overnight under nitrogen gas. After reaction, the solution was poured over 150 mL of 2 M HCl and extracted with EtOAc (2 ×100mL). the combined solution was dried over anhydrous sodium sulfate and concentrated under reduced pressure to give dark brown oil that was purified by using column chromatography (20% EtOAc/Hexane) with yield of 75%. 1H NMR (300 MHz, CDCl3): 4.1 (s, 4H), 5.9 (s, 1H), 7.24 (s, 1H), 7.5 (d, 2H, J = 7.7), 7.7 (d, 2H, J = 7.1), 8.1 (s, 1H); 13C NMR (300 MHz, CDCl3): 58.6, 65.5, 99.9, 123.7, 127, 128.4, 129.4, 132.5, 135.6, 137.9, 139.2, and 147.9.

Synthesis of compound diethyl-6-chloro-5-nitronaphthalene-2,3-dicarboxylate (14): 4-chloro-3-nitro-2-(phenylsulfonylmethyl) benzaldehyde (13) (0.6 g, 1.7 mmol), diethylmaleate (310 mg, 2.0 mmol), and 18-crown-6 (30 mg, 0.11 mmol) was dissolved in acetonitrile (100 mL) then potassium carbonate (1.2 g) was added to the solution and the resulting mixture was stirred for 0.5 h. The reaction was refluxed over night, then filtered over celite and concentrated under reduced pressure. The resulting dark oily residue was purified by column chromatography (30% EtOAc/Hexane) to give the desired product. (0.45 g, 76% yield). 1H NMR (300 MHz, CDCl3): 1.24 (t, 6H, J = 7.1), 7.9 (d, 1H, J = 8.0), 8.5 (s, 1H), 9.0 (s, 1H); 13C NMR (300 MHz, CDCl3): 14.6, 66.9, 115.9, 126.1, 127.2, 129.1, 131.3, 135.8, 155.9, and 174.1.

Synthesis of compound 15: Compound 14 (60 mg, 0.22 mmol) and p-diaminophenylene (26 mg, 0.24 mmol) was dissolved in pyridine and refluxed overnight. The solution was concentrated under reduced pressure and purified by column chromatography (80% EtOAc/Hexane) to give final product 15 with yield of 95%. 1H NMR (300 MHz, DMSO-d6): 6.9 (s, NH2, 2H), 7.1 (s, 2H), 7.3 (s, 2H), 7.5 (d, 1H, J = 8.6), 8.1 (d, 1H, J = 7.6), 8.4 (s, 1H), 9.9 (s, 1H). 13C NMR (300 MHz, CDCl3): 114.1, 117.8, 124.1, 125.2, 128.6, 129.5, 130.2, 132.8, 134.6, 136.5, 149.3, and 167.5.

Fluorescence Lifetime decay plots

Figure S1. Fluorescence lifetime of F-OCH3 in dichloromethane (on the left) and in acetonitrile (on the right) with excitation at 310 nm with concentration of 50 uM

Hexane, SW Emission

Toluene, SW Emission

EtOAc, SW Emission

Figure S2 SW emission lifetime of F-2OCH3 in hexane (on the top), toluene (in the middle), and in ethyl acetate (on the bottom) with excitation at 310 nm with concentration of 50 uM

Figure S3 LW emission lifetime of F-2OCH3 in hexane excitation at 370 nm with concentration of 50 uM.

Figure S4. LW emission lifetime of Cl-NH2 in hexane excitation at 370 nm with concentration of 50 uM.

Figure S5. LW emission lifetime of NO2/Cl-NH2 in hexane excitation at 370 nm with concentration of 50 uM.

Figure S6. LW emission lifetime of NO2/Cl-NH2 in hexane excitation at 405 nm with concentration of 50 uM

Multi-exponential fitting in the form:

ax values are the relative amplitudes (%);  ax = Ax*tx

Lifetimes, tx, are given in units of ns

| Sample | 1 | 1 | 2 |  | 3 |  | 4 |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| F-2OCH3 | 63 | 1.21 | 27 | 2.83 | 10 | 8.22 |  |  |
| Cl-NH2 | 22 | 1.17 | 23 | 2.84 | 5 | 7.32 | 39 | 13.8 |
| NO2/Cl-NH2 (390 NanoLED) | 19.2 | 0.11 | 43 | 1.06 | 39 | 3.68 | 21 | 16.4 |
| NO2/Cl-NH2 (405 Delta Diode laser) | 7 | 0.49 | 19 | 1.02 | 59 | 4.19 | 18 | 9.68 |

Table S1 Absorbance maxima of F-OCH3 in solvents of various polarities

| Solvents | f | SW (/nm) | LW (/nm) |
| --- | --- | --- | --- |
| Cyclohexane | 0 | 339 | 357 |
| Hexane | 0 | 338 | 356 |
| Toluene | 0.013 | 343 | 362 |
| 1,4-Dioxane | 0.03 | 342 | 360 |
| Anisole | 0.11 | 345 | 364 |
| Bromobenzene | 0.13 | - | 363 |
| CHCl3 | 0.148 | 347 | 365 |
| Chlorobenzene | 0.19 | - | 362 |
| EtOAc | 0.200 | 343 | 359 |
| CH2Cl2 | 0.217 | 346.5 | 363 |
| DMSO | 0.263 | 344 | 362 |
| Acetone | 0.284 | - | 359 |
| Acetonitrile | 0.305 | 344 | 362 |

Table S2 Fluorescence maxima of F-OCH3 in solvents of various polarities

| Solvents | f | SW (/nm) | LW (/nm) |
| --- | --- | --- | --- |
| Cyclohexane | 0 | 355 | 508 |
| Hexane | 0 | 358 | 513 |
| Toluene | 0.013 | 361 | 530 |
| 1,4-Dioxane | 0.03 | 372 | 528 |
| Anisole | 0.11 | 377 | 534 |
| Bromobenzene | 0.13 | 372 | 528 |
| CHCl3 | 0.148 | 378 | 517 |
| Chrolobenzene | 0.19 | 369 | 522 |
| EtOAc | 0.200 | 374 | 518 |
| CH2Cl2 | 0.217 | 376 | 521 |
| DMSO | 0.263 | 363 | 530 |
| Acetone | 0.284 | 365 | 524 |
| Acetonitrile | 0.305 | 361 | 524 |

Table S3 Absorbance maxima of F-2OCH3 in solvents of various polarities

| Solvents | f | SW (/nm) | LW (/nm) |
| --- | --- | --- | --- |
| Cyclohexane | 0 | 338 | 354.5 |
| Hexane | 0 | 338 | 354 |
| Toluene | 0.013 | 345 | 358 |
| 1,4-Dioxane | 0.03 | 342 | 354 |
| Anisole | 0.11 | 345 | 358 |
| Bromobenzene | 0.13 | - | 360 |
| CHCl3 | 0.148 | 347 | 361 |
| Chlorobenzene | 0.19 | 345 | 358 |
| EtOAc | 0.200 | 340 | 354 |
| CH2Cl2 | 0.217 | 345 | 358 |
| DMSO | 0.263 | 342 | 358 |
| Acetonitrile | 0.305 | 341 | 356 |

Table S4 Fluorescence maxima of F-2OCH3 in solvents of various polarities

| Solvents | f | SW (/nm) | LW (/nm) |
| --- | --- | --- | --- |
| Cyclohexane | 0 | 355 | 506 |
| Hexane | 0 | 373 | 506 |
| Toluene | 0.013 | 390 | 610 |
| Dioxane | 0.03 | 392 |  |
| Anisole | 0.11 | 396.5 |  |
| CHCl3 | 0.148 | 393 | - |
| Chlorobenzene | 0.19 | 394.5 | - |
| EtOAc | 0.200 | 391 | - |
| CH2Cl2 | 0.217 | 393 | - |
| DMSO | 0.263 | 398 | - |
| Acetonitrile | 0.305 | 395 | - |

Figure S7 Absorption spectra of F-OCH3 in solvents of varying polarities

Figure S8. Fluorescence spectra of F-OCH3 in solvents of varying polarities, excitation at 310 nm at concentation of 10 uM

Figure S9. Absorption spectra of F-2OCH3 in solvents of varying polarities

Figure S10. Fluorescence spectra of F-2OCH3 in solvents of varying polarities, excitation at 310 nm at concentation of 10 uM

Stacked plots of Absorption spectra for F-2OCH3 in hexane

Methodology to develop a WOLED device

To evaluate these N-aryl-NIs suitability for solid-state electroluminescence, investigation into their solid-state photoluminescent behavior provides a good first approximation prior to device fabrication.  The investigated organic compounds were deposited onto pre-cleaned glass slides by high-vacuum thermal deposition for F-OCH3 and F-2OCH3. For Cl-NH2 and NO2/Cl-NH2, thermal deposition failed to deposit as thin films on the glass slides because of their high melting points (>400 °C) and strong intermolecular interactions. Therefore, thin films of Cl-NH2 and NO2/Cl-NH2 were obtained by spraying the solutions onto glass slides.

### Comparison of the absorbance of these compounds in solution and thin film

The net absorbance of these compounds as thin films on the glass slides was obtained by subtracting the absorbance of the blank glass slide from the absorbance of the compounds as thin film on the glass slides. The absorbance of these dyes was obtained from a solution with the concentration of 10-5 M. The specific solvents for each compound were chosen in order to maximize dual-emission or panchromatic emission. The absorption spectra of these compounds both in various solutions and thin films (or solid state) are shown below in Figure S11.

Figure S11. Comparative absorbance spectra of the compounds in both solution and thin film

From figure S11, the absorbance maximum of F-OCH3 is centered at 359 nm in ethyl acetate, and the absorbance maximum of F-OCH3 in thin film format is about 390 nm. The absorbance maximum of F-OCH3 showed about a 30 nm red-shift. The absorbance maximum of F-2OCH3 in cyclohexane is centered at 353 nm, and the absorbance maximum in thin film red-shifted about 15 nm to 368 nm. Such red-shifts are typically attributed to increased stacking interactions in the solid-state; thereby lowering the energy between π-π*.1 As figure S11 illustrates, it becomes difficult to identify the absorbance maxima of both NO2/Cl-NH2 and Cl-NH2. For NO2/Cl-NH2, the absorbance at 495 and 510 nm peaks almost disappear from the thin film absorbance spectrum. To summarize these observations, solvent effects such as solvent-separated species appears to cause the absorbance shifts of these two peaks in solution relative to the solid state.

Figure S12. Fluorescence of the materials in both solution and thin film.

The fluorescence spectra of these compounds both in solutions and in thin films are shown in Figure S12. The fluorescence maximum at the short wavelength of F-OCH3 peaks at 374 nm in ethyl acetate whereas the fluorescence maximum at the short wavelength of F-OCH3 in thin film occurs at 400 nm. The fluorescence maximum at the longer wavelength of F-OCH3 in solution peaks at 518 nm, a broad shoulder of longer wavelength emission from F-OCH3 in thin film appears at 550 nm. The bathochromic shifts for the short wavelength and the longer wavelength fluorescence maxima in solution and thin film range between 26 and 32 nm, respectively. For F-2OCH3, the red-shifts for both the short wavelength and the longer wavelength fluorescence maxima are about 20 nm and 48 nm, respectively. This red-shift could be attributed to increased stacking interactions of the fluorophores in the solid state. The dual-fluorescence of F-OCH3 and F-2OCH3 displayed in thin films provides results on the promising panchromatic emission for electroluminescence. For NO2/Cl-NH2, the short wavelength maximum in thin film was red-shifted about 20 nm compared to solution phase. In addition, comparing the spectra of NO2/Cl-NH2 in solution to the thin film, the broad fluorescence spectrum in the thin film disappeared. In comparison to a much broader peak for Cl-NH2 in solution, the fluorescence of the corresponding thin film sample was reduced to mono-fluorescent behavior. The fluorescence maximum of Cl-NH2 was blue-shifted about 45 nm in thin film. The reason behind the blue-shift in the Cl-NH2 thin film is unknown at this point. The fluorescence peaks in both solution and thin films are listed in Table S5.

Table S5. Absorption and fluorescence of the compounds in solution and thin film

| Compd. | Solution |  | Thin film |  | Optical band gapa (Egopt) (eV) |
| --- | --- | --- | --- | --- | --- |
|  | Absor. max; onset (nm) | PL. max (nm) | Absor. max (nm) | PL. max (nm) |  |
| F-OCH3 | 359; 375 | 374, 518b | 398 | 400, 550 | 3.3 |
| F-2OCH3 | 354; 440 | 335, 554c | 369 | 405, 602 | 2.8 |
| Cl-NH2 | 360; 375 | 442, 525 d |  | 397 | 3.3 |
| NO2/Cl-NH2 | 365; 538 | 444, 463, 492, 520, 595e |  | 456, 470 | 2.3 |

a: the optical band gap was calculated with the equation: Egopt=1240 (eV∙nm)/λonset (nm)

b: measured in EtOAc; c: cyclohexane; d: methanol; e: water.

Molecular Orbitals: HOMO and LUMO energies measurement

The onset values for oxidation and reduction potentials determined vs. Ag/Ag+ are presented in Table S6. F-OCH3, F-2OCH3, Cl-NH2, and NO2/Cl-NH2 show a reversible one-electron reduction process with the onset potential of -1.69, -1.71, -1.82, and -1.25 V relative to ferrocene, respectively. The energy level of Fc/Fc+ was assumed at - 4.8 eV to the vacuum.2  The CV of the investigated compounds was plotted with respect to Ag/Ag+ vs Fc/Fc+. The calculated HOMO, LUMO, and the band gaps are listed in Table S6. Equations used to calculate these terms are listed below.

EHOMO=-Eonsetox+4.8 eV                                       (eq. 4-1)

ELUMO=-Eonsetre+4.8 eV                                       (eq. 4-2)

Table S6. The band gap energies of the investigated compounds

| Compd. | Ere/onset (V) | Eox/onset (V) | Ip (LUMO) (eV) | Ea (HOMO) (eV) | Band gap (EgCV) (eV) |
| --- | --- | --- | --- | --- | --- |
| F-OCH3 | -1.69 | 0.12 | -3.11 | -4.92 | 1.81 (3.3)a |
| F-2OCH3 | -1.71 | 0.06 | -3.09 | -4.96 | 1.77 (3.2)a |
| Cl-NH2 | -1.82 | 0.25 | -2.98 | -5.05 | 2.07 (3.3)a |
| NO2/Cl-NH2 | -1.25 | 0.09 | -3.55 | -4.89 | 1.34 (2.3)a |

a: The data in the parenthesis are optical band gaps determined from absorbance spectra.

The energy gaps of these materials determined by cyclic voltammetry are quite different from those measured by the spectroscopic method; the data comparison of the two methods is shown in Table S6. The energy differences obtained with these two methods exceeded 1 eV for FOCH3, F-2OCH3, Cl-NH2, and NO2/Cl-NH2. However, the trending of these two methods is consistent. For example, NO2/Cl-NH2 exhibited the smallest band gap, and Cl-NH2 possesses the largest band gap. Compared with the work function of the common cathode LiF/Al (3.4 eV), the LUMO energies of these materials listed in table S6 showed a small energy difference of less than 0.45 eV. The HOMO energies of these materials are very close together with a difference of about 0.15 eV. With respect to the work function of the anode ITO (4.7 eV), they also showed a very small difference of less than 0.3 eV. In terms of the energy barrier, these results indicate that these materials provide promising charge injection and transport functions.

References

- Tang, W.; Huang, D.; He, C.; Yi, Y.; Zhang, J.; Di, C.; Zhang, Z.; Li, Y. Solution-Processed Small Molecules Based on Indacenodithiophene for High Performance Thin-Film Transistors and Organic Solar Cells. Organic Electronics 2014, 15, 1155-1165.

- Nandhikonda, P.; Heagy, M. D. Dual Fluorescent N-Aryl-2,3-Naphthalimides: Applications in Ratiometric DNA Detection and White Organic Light-Emitting Devices. Org. Lett. 2010, 12, 4796-4799.

- Deng, P.; Liu, L.; Ren, S.; Li, H.; Zhang, Q. N-Acylation: An Effective Method for Reducing the LUMO Energy Levels of Conjugated Polymers Containing Five-Membered Lactam Units. Chem. Commun. 2012, 48, 6960-6962.

- Huang, J.; Hou, W.-J.; Li, J.-H.; Li, G.; Yang, Y. Improving the Power Efficiency of White Light-Emitting Diode by Doping Electron Transport Material. Appl. Phys. Lett. 2006, 89, Article number:133509.