Efficient production of formic acid by simultaneous photoreduction of bicarbonate and oxidation of glycerol on gold-TiO2 composite under solar light

Hanqing Pan†, Alexzander Steiniger‡, Michael D. Heagy†, *Sanchari Chowdhury‡ᵩ

†Department of Chemistry, ‡Department of Chemical Engineering, ᵩ Material Science and Engineering, New Mexico Institute of Mining and Technology

Socorro, NM 87801

Supporting Information

Ion Chromatography for formate analysis:

Ion chromatography is used to separate out a particular analyte in a mixture. Each analyte elutes at a specific retention time. From the chromatography column, the analyte of interest (formate) is displaced by the eluent (0.4 mM heptafluorobutyric acid). With each injection, a chromatogram is generated – a plot of detector signal output versus time. The chromatogram shows the elution times of different anions; in particular, the formate anion has a retention time of approximately 8 minutes. The concentration of each injection is proportional to peak area and height. Before each run, a calibration curve is first generated by injecting 0, 5, 15, 25, 50, 100, and 150 ppm of a standard formic acid solution (Fig. s6). The instrument then uses this data to create a linear offset curve, used to determine the concentration of each injection. To analyze the data, the instrument integrates the peak area, and based on the linear offset calibration curve, injection concentration (in ppm) is obtained. A sample chromatogram is shown below in Fig. s5.

Figure s1. Sample ion chromatography chromatograph.

Figure s2. Formic acid standard curve. Points shown are the averaged results of three separate injections.

Figure s3. Diffuse reflectance spectrum and Kubelka-Munk treated plot of TiO2.

Wavelength (nm)

Absorbance

Absorbance

Wavelength (nm)

TiO2-gold visible light

TiO2  visible light

Wavelength (nm)

Absorbance

Absorbance

Wavelength (nm)

TiO2 365 nm light

TiO2-gold 365 nm light

Figure s4  Resazurin reduction  with TiO2 and TiO2-gold composite under visible light and 365 nm light

Wavelength (nm)

365 nm light

Absorbance

Wavelength (nm)

Figure s5: Hydroxyl radical generation as probed by the emission of HTA when excited with 340 nm light. Emission peak of HTA after 1hour 365 nm light exposure in TiO2 solution is normalized to one. Other emission spectra are scaled accordingly.

Calculation of apparent quantum efficiency (AQE)

To calculate AQE, by using an Ophir Photonics Nova II laser energy meter, the energy output of the solar simulator was measured (1000 W/m2). This power measurement was converted to moles of photons per second. This photon flux was then used to calculate the apparent quantum efficiency (AQE) of the catalyst using equations (1) and (2).

n mol photons ∙ 1 mol e-mol photons  ∙ mol formate2 mol e- =theoretical        (1)

actual mol formatetheoretical mol formate  ∙100 =%AQE         (2)

The surface area of the quartz tube is 0.00195 m2.

365 nm

Reference: CM paper

First we convert solar flux to photons per second. Since 1 W = 1 J/s, at 365 nm:

E= hcλ= 1.24x103 eV∙nm365 nm ∙ 1.602x10-19J1 eV=5.44x10-19 J

1000Jsm2∙photon5.44x10-19J=1.83x1021photonss/m2

Multiplying by the surface area we obtain:

1.83x1021photonssm2 ∙0.00195 m2=3.56x1018 photons/s

By taking into account that our experiment is over 8 hours and converting to moles of photons, we have calculated that 5.04x10-2 mol photons is the theoretical value.

3.56x1018photonss ∙ 60s1min ∙ 60min1hr ∙8hr ∙ 1mol6.02x1023 photons=0.17 mol photons

By using Eqn. 1 we calculate the theoretical moles of formate:

0.17 mol photons ∙ 1 mol e-mol photons  ∙ mol formate2 mol e- =0.085 mol formate (theoretical)

To calculate the actual moles of formate we convert our formate value from ion chromatography (in ppm) to moles. Using the example of TiO2 under 365 nm irradiation, which produced 319 ppm of formate, it is converted to 0.007 moles, then using Eqn. 2:

0.007 actual mol formate0.085 theoretical mol formate ∙100=8.34%

Solar irradiation

Reference: chapter 2??

By determining the area of the curve of the solar spectrum, we find that the number of photons is 5.25x1021 photons/s/m2. We multiply this by the surface area of the quartz tube and account for 8 hours of irradiation.

5.25x1021photonssm2∙0.00195 m2=1.02x1019photonss

1.02x1019photonss ∙ 60s1min  ∙ 60min1hr ∙8hr ∙ 1mol6.02x1023photons=0.489 mol photons

0.489 mol photons ∙ 1 mol e-mol photons ∙ mol formate2 mol e-=0.244 mol formate (theoretical)

To calculate the actual moles of formate we convert the ppm formate value to moles. Using the example of TiO2 under solar irradiation, which produced 33 ppm of formate, it is converted to 0.000733 moles formate. By using Eqn. 2:

0.000733 actual mol formate0.244 theoretical mol formate ∙100= 0.30%